**Andrew Casto**

Assistant Professor, Ceramics

The University of Iowa

andycasto@gmail.com

937-570-0750  |  www.andrewcasto.com

Glaze Recipes – Fall 2016 – Cone 6 oxidation or reduction

1. **Matte White**

Batch Bucket

Frit 3124 35 7000g

EPK 34 6800g

Wollastonite 26 5200g

Silica/Flint 5 1000g

100% 20,000g

+

Zircopax 5% 1000g

1. **Matte Blue/Green**

Batch Bucket

Frit 3124 35 7000g

EPK 34 6800g

Wollastonite 26 5200g

Silica/Flint 5 1000g

100% 20,000g

+

Red Iron Ox. 1.5% 300g

Cobalt Carb. .5% 100g

Copper Carb. 1% 200g

1. **Matte Yellow**

Batch Bucket

Frit 3124 35 7000g

EPK 34 6800g

Wollastonite 26 5200g

Silica/Flint 5 1000g

100% 20,000g

+

Zircopax 5% 1000g

Mason stain 6% 1200g

6450 Praseodymium

Yellow

1. **Tenmoku**

Batch Bucket

Frit 3134 33.5% 6700g

Frit 3195 26% 5200g

OM4 Ball 17% 3400g

Silica/Flint 23.5% 4700g

100% 20,000g

Red Iron Ox. 12.5% 2,500g

Rutile 1% 200g

1. **Gloss Clear**

Batch Bucket

EPK 20% 4000g

Silica/Flint 20% 4000g

Wollastonite 20% 4000g

G200 Feldspar 20% 4000g

Frit 3134 20%. 4000g

100% 20,000g

1. **Gloss Copper Green/Red**

Batch Bucket

EPK 20% 4000g

Silica/Flint 20% 4000g

Wollastonite 20% 4000g

G200 Feldspar 20% 4000g

Frit 3134 20%. 4000g

100% 20,000g

Copper Carbonate 4% 800g

1. **Gloss Blue**

Batch Bucket

EPK 20% 4000g

Silica/Flint 20% 4000g

Wollastonite 20% 4000g

G200 Feldspar 20% 4000g

Frit 3134 20%. 4000g

100% 20,000g

Cobalt Carbonate 4% 800g

1. **Gloss White**

Batch Bucket

EPK 20% 4000g

Silica/Flint 20% 4000g

Wollastonite 20% 4000g

G200 Feldspar 20% 4000g

Frit 3134 20%. 4000g

100% 20,000g

Zircopax 10% 2000g